21 Roberts St West., Osborne Park, Western Australia 6017    Phone (61) 08 9242 2990   Fax  (61) 08 9242 4867

KRAFT KOTE TECHNICAL INFORMATION

KRAFT KOTE IS A SELF LEVELLING, HIGH GLOSS 2 PART EPOXY RESIN. IT IS A HIGHLY VERSATILE

LIQUID COATING THAT HARDENS TO PRODUCE A THICK, CLEAR, DURABLE AND GLOSSY FINISH

KRAFT KOTE SHOULD BE MIXED BY VOLUME WITH EQUAL PARTS OF RESIN AND HARDENER IN A CLEAN,

PLASTIC MEASURING CONTAINER. THE PRODUCT SETS QUICKLY AND PRODUCES A HARD FINISH WHEN

CURED.

THE KIT CONTAINS EQUAL QUANTITIES OF RESIN AND HARDENER.

1 LITRE OF KRAFT KOTE COVERS APPROXIMATELY 1.1 SQUARE METRES OF SURFACE AREA.

MAKE SURE THE SURFACE OF THE TABLETOP IS CLEAN, FREE OF OILS, SOLVENTS AND DUST.

WE RECOMMEND PLACING A COVER ABOVE YOUR TIMBER TO PROTECT FROM DUST PARTICLES.

THOROUGHLY MIX EQUAL PARTS OF RESIN AND HARDENER IN A CLEAN CONTAINER.

POUR THE MIX ONTO THE SURFACE AND SPREAD WITH A CLEAN, HIGH QUALITY BRUSH.

USE A HEAT GUN TO DRAW BUBBLES TO THE SURFACE.

LIGHTLY BRUSH OVER THE LIQUID TO SPREAD.

LEAVE TO CURE.